LGS WFS Optics Specifications

Document Number: E-MAO-PL0-IPA-SPE-104

Document Version: 01D3

Document Type: SPE

Released On: 2024-12-16

|  | Name | Signature | Date |
| --- | --- | --- | --- |
| Owner: | Patrick Rabou |  | 2024-12-16 |
| Approved by SI: | Laurent Jocou |  | 2024-12-16 |
| Released by PM: | Manal Chebbo |  | 2024-12-16 |

Authors

| Name | Affiliation |
| --- | --- |
| Patrick Rabou (Optics) | IPAG |
| Laurent Jocou (System) | IPAG |

Change Record from previous version

| Date | Affected Section(s) | Changes / Reason / Remarks |
| --- | --- | --- |
| 2024-09-27 | All | First draft issue. |
| 2024-10-15 | 4.5, 4.5, 6.4 7.1 | Added mirrors specifications. Added coatings simulations. |
| 2024-11-19 | 1.2, 4.5 | Change the drawing, PSM mirror geometry |
| 2024-12-16 | 4.1, 5.1 4.5 | Added Assembly Drawings PSM Mirror Mechanical Drawing |
| 2024-12-17 |  | Change of Document number |

Contents

1.	Introduction	5

1.1	Scope	5

1.2	LGSWFS Module overview	5

2.	Related Documents	7

2.1	Applicable Documents	7

2.2	Reference Documents	7

3.	General Optics Specifications	8

3.1	Environment Specifications	8

3.2	Optical Materials Specifications	8

3.3	General Coatings Specifications	8

3.3.1	SLAR_589 Coating Specifications	9

3.3.2	VAR_589 Coating Specifications	9

3.3.3	NBP_589_10 (Bandpass + Blocking) Coating Specifications	9

3.3.4	HRD_589_120 Coating Specifications	9

3.3.5	BCR_589 Coating Specifications	9

3.4	Cleanliness Specifications	9

3.5	ISO 10110 Specifications	10

4.	Collimator Optics Specifications	11

4.1	COL Collimator Optical Assembly	11

4.2	COL Collimator Doublet (COL_L1+COL_L2)	13

4.2.1	COL Collimator Doublet Lens 1 (COL_L1)	14

4.2.2	COL Collimator Doublet Lens 2 (COL_L2)	15

4.3	COL Collimator Lens 3 (COL_L3)	16

4.4	COL Narrow Bandpass Filter (COL_NBPF)	17

4.5	COL Folding Mirror 1 (COL_FM1)	18

4.6	COL Folding Mirror 2 (COL_FM2)	20

5.	Detector Module Relay Optics Specifications	21

5.1	LDM Relay Optical Assembly	22

5.2	LDM Relay Lens 1 (LDM_L1)	24

5.3	LDM Relay Lens 2 (LDM_L2)	25

5.4	LDM Relay Lens 3 (LDM_L3)	26

5.5	LDM Relay Lens 4 (LDM_L4)	27

5.6	LDM Relay Lens 5 (LDM_L5)	28

5.7	LDM Relay Lens 6 (LDM_L6)	29

6.	Calibration Unit Optics Specifications	30

6.1	CAL Relay Optical Assembly	30

6.2	CAL Cemented Doublet (CAL_L1+CAL_L2)	32

6.2.1	CAL Cemented Doublet Lens 1 (CAL_L1)	33

6.2.2	CAL Cemented Doublet Lens 2 (CAL_L2)	34

6.3	CAL Pupil Mask (CAL_PM)	35

6.3.1	CAL Pupil Mask Plate	35

6.3.2	CAL Pupil Mask Shape	36

6.4	CAL Folding Mirror (CAL_FM)	37

7.	Annex	38

7.1	Coatings preliminary Design	38

7.1.1	SLAR_589 Coating Design	38

7.1.2	VAR_589 Coating Design	38

7.1.3	NBP_589_10 (Bandpass + Blocking) Coating Design	38

7.1.4	HRD_589_120 Coating Design	39

7.1.5	BCR_589 Coating Design	39

7.1.6	Total LGS WFS Coatings Transmission	39

List of Figures

Figure 1-1. Cut-through of a single LGS WFS channel	6

Figure 4-1. COL Collimator Optical Assembly Drawing	11

Figure 4-2. COL_FM1 Mechanical Drawing	19

Figure 5-1. Cross-section of a single LDM	21

Figure 5-2. LDM Optical Assembly Drawing	22

Figure 6-1. CAL Calibration Unit Optical Assembly Drawing	30

Figure 7-1. NBP Filter Coating Simulations Transmission	38

Figure 7-2. BCR Coating Simulations Transmission / Total Optical Density	39

Figure 7-3. LGS Probe Coatings Simulations Transmission / Total Optical Density	40

Figure 7-4. Calibration Coatings Simulations Transmission / Total Optical Density	40

List of Tables

Table 4-1. COL Collimator Prescription	11

Table 5-1. LDM Relay Prescription	22

Table 6-1. CAL Calibration Unit Prescription	30

# Introduction

## Scope

This document describes the manufacturing specifications of the MORFEO LGSWFS optics.

## LGSWFS Module overview

MORFEO is a first-generation instrument for the Extremely Large Telescope (ELT). The instrument aims to compensate for the distortion of light caused by atmosphere turbulence. The instrument will use several natural guide stars around the scientific field-of-view and 6 laser guide stars (LGS) to provide the required image quality for the two scientific instruments fed by MORFEO.

In MORFEO, the Institute for Planetary sciences and Astrophysics of Grenoble (IPAG) is responsible of the development of the MORFEO LGSWFS Module.

The LGSWGS Module – called PL0 – which consists mainly of 6 Shack-Hartman wavefront sensors mounted on a rotating and translating platform in order to follow the telescope’s elevation.

Each individual WFS – also called WFS channel – is composed of:

- A pick-off mirror which folds the beam

- A field-stop in the ELT’s LGS focal plane

- A narrow-band filter centered on the sodium wavelength (λ=589nm)

- A collimator that images the ELT pupil

- A lenslet array that samples the ELT pupil into sub-apertures and forms images of the LGS (the lenslet array is not in the components to be manufactured and specified in this document)

- A relay optic that transports the images of the LGS formed by the lenslets onto the detector

- A CMOS detector that reads the spots and sends the images to the AO RTC

The rotating and translating support is mainly composed of:

- A motorized rotation stage and angular position sensor that holds the 6 WFS and that follows the telescope’s elevation angle

- A vertical translation stage that holds the rotation stage and allows to move the WFS input focus to the focal plane to the LGS provided by the MORFEO optical path

- A calibration unit can send light into each WFS and can be removed from the optical path during observations

- An interface frame holds the translation stage on one side and is fixed to the MORFEO main structure on the other side

Camera

Lenslet

Array

Relay

Collimator

Pupil

Steering

Mirror

Figure 1-1. Cut-through of a single LGS WFS channel

# Related Documents

## Applicable Documents

The following applicable documents form a part of the present document to the extent specified herein. In the event of conflict between applicable documents and the content of the present document, the content of the present document shall be taken as superseding.

Common Requirements for ELT Instruments
ESO-254547 Version 3

Common ICD between the ELT Nasmyth Instruments and the Rest of the ELT System ESO-253082 Version 4

LGSWFS Technical Specifications
E-MAO-PL0-INA-SPE-003

ZEMAX file for ELT Optical Design Specification
ESO-254351 Version 2

Standard Coordinate Systems and Basic Conventions
ESO-193058 Version 6

Relevant Atmospheric Parameters for ELT AO Analysis and Simulations
ESO-258292 Version 2

MORFEO Calibration Units User Requirements
E-MAO-000-ESO-TNO-002 Version 2D4

ICD between the WFS Cameras and the ELT Instruments
ESO-302894 Version 2

Instrument Control Hardware Guidelines for MORFEO Subsystems 
E-MAO-PH0-INA-TNO-001 1D4

MORFEO LGS WFS Optical Design ZEMAX file
MORFEO LGSWFS Module_PDR1_2021-03-01.zmx

## Reference Documents

The following documents, of the exact version shown herein, are listed as background references only. They are not to be construed as a binding complement to the present document.

LGS WFS Module Analysis Report
E-MAO-PL0-IPA-ANR-013 Version 2

MORFEO LGSWFS Interface Control Document
E-MAO-PL0-IPA-ICD-014 version 1

# General Optics Specifications

The supplier is invited to propose alternate specifications, if some are not reachable by the manufacturing process, or if they lead to excessive costs to be reached.

If some tests are not possible for the supplier, or if they lead to excessive costs, these tests will be done by IPAG and the acceptance will be done after validation of these tests.

All specified dimensions shall be measured with a 0.01 mm accuracy and reported.

Radii of curvature and thickness will be adjusted to manufacturer available machining and control tools and glass melt data by IPAG, when possible.

## Environment Specifications

The environment specifications for nominal operation of MORFEO are the following:

- Functional air temperature range:			-10 to +30 °C

- Operational air temperature range: 			+0 to +20 °C

- Air temperature gradient at night: 			1.4 °C/hour

- Humidity: 						0 to 95 %

- Transport and storage air temperature range: 	-15 to +55 °C

## Optical Materials Specifications

- All specified lenses shall be manufactured from the same glass melt.

- Glass melt data shall include refractive index measurements at standard visible wavelengths (C, d, F lines at least).

## General Coatings Specifications

See section 7.1 for a preliminary design study of the coatings.

- Coating design should minimize stress on surface (coated surface sagitta error should reach the component surface sagitta error or radius of curvature error specification).

- Coatings shall be optimized for reference wavelength 589.3 nm (sodium doublet line) and specified angle of incidence range.

- Coating Reflectivity shall be measured on minimum spectral band [530-650] nm, as close as possible to specified angle of incidence.

- Component surface scratch and dig specification apply to coated surface.

- Coating durability:  comply with MIL-C-675, MIL-C-48497, MIL-M-13508, DIN  58197 (where applicable).

### SLAR_589 Coating Specifications

Single Layer MgF2 anti-reflection coating, normal incidence (0°)

Substrate: S-LAH95 (Ohara)

Reflectivity at 589.3 nm: RABS < 0.25 %

Reflectivity [570-610] nm: RAVG < 0.5 %

### VAR_589 Coating Specifications

V anti-reflection coating, normal incidence (0°)

Substrates: S-BSL7, S-TIM25 (Ohara), Borofloat ® (Schott), Fused Silica (coating design to be adjusted to substrate refractive index when needed to reach specification)

Reflectivity at 589.3 nm: RABS < 0.25 %

Reflectivity [570-610] nm: RAVG < 0.5 %

### NBP_589_10 (Bandpass + Blocking) Coating Specifications

Narrow Band Pass coating, Central Wavelength 589 nm, FWHM 10 nm

In converging F# 5 beam, 28.4 % linear central obscuration (cone half angle 1.6° to 5.7°)

Incidence < 0.3°, working temperature range [0, 20] °C

Substrates: Borofloat ® (Schott) or Fused Silica

Substrate should be anti-reflection coated (VAR_589) to minimize ghost level at 589.3 nm (ghost level < 0.05 % (goal 0.01 %) of direct transmitted beam)

In Band Transmission [586-592] nm: TAVG > 95 %, TABS > 90 %, TABS > 96 % at 589.3 nm

Out Band Transmission [400-580] + [598-900] nm: TABS < 10 %, TAVG < 0.05 % (goal 0.01 %)

### HRD_589_120 Coating Specifications

High Reflectivity Dielectric Mirror coating, incidence 45 ± 6°

Substrates: S-BSL7 (Ohara), Fused Silica

Reflectivity [584-594] nm: RAVG > 99.5 %, RABS > 99 %

Reflectivity [530-650] nm: RABS > 50 %

Reflectivity [800-1200] nm: RABS < 5 % (Cold Mirror, Long Wave Pass design)

### BCR_589 Coating Specifications

Black Chrome Reflective coating, normal incidence (0°)

Substrates: Fused Silica

Reflectivity [584-594] nm: RABS < 1.0 %, TABS < 0.01 % (TBC)

Reflectivity [570-610] nm: RAVG < 10.0 %

## Cleanliness Specifications

Dust contamination is an issue for the optical components.

Any non-removable dust particle shall be counted as the equivalent scratch/dig in the specification.

Optics shall be delivered cleaned in an adapted packaging.

Dust particles removal shall be part of the coatings cleaning procedure.

## ISO 10110 Specifications

Specification and control atmospheric conditions are temperature 20°C and pressure 1013 hPa.

Unless otherwise specified, reference wavelength is λ = 546.07 nm (green mercury line).

Opto-mechanical specifications follow ISO 10110 specifications format:

| Part 2: Material imperfections - Stress birefringence |  |  |
| --- | --- | --- |
| 0/ | A | A: max OPD (nm/cm) |
| Part 3: Material imperfections - Bubbles and inclusions |  |  |
| 1/ | NxA | N: number of bubbles A: bubble grade number |
| Part 4: Material imperfections - Inhomogeneity and striae |  |  |
| 2/ | A; B | A: homogeneity class B: striae class |
| Part 5: Surface form tolerances Surface form error specification is in fringes (half wavelength) unit |  |  |
| 3/ | A (B/C) RMSx < D; λ = E | A: maximum permissible sagitta error B: maximum permissible irregularity C: maximum permissible rotationally symmetric irregularity D: maximum permissible rms quantity of type x (x is t: total rms deviation, i: rms irregularity, or a: rms asymmetry) E: reference wavelength (nm) |
| Part 6: Centering tolerances |  |  |
| 4/ | σ | σ: surface tilt angle (minutes (‘) or seconds (‘’)) |
| Part 7: Surface imperfection tolerances |  |  |
| 5/ | NxA; CN’xA’; LN’’xA’’; EA’’’ | N: number of allowed general imperfections, A: defect grade number (mm) N’: number of coating blemishes, A’: coating blemish grade number (mm) N’’: number of long scratches (> 2 mm), A’’: maximum width of scratch (mm) A’’’: maximum extend of edge chips (mm) |
| Rq A D B / C Part 8: Surface texture |  |  |
|  |  | A: rms surface roughness (µm) B / C: measurement between sampling lengths B and C (mm) D = G for ground surfaces, Px for polished surfaces (x: polishing grade number) |
| λ Part 9: Surface treatment and coating |  |  |
|  | A | A: coating specification reference |
| Part 14: Wavefront deformation tolerance Wavefront error specification is single-pass, in wavelengths unit |  |  |
| 13/ | A (B/C) RMSx < D; λ = E | A: maximum permissible wavefront sagitta error B: maximum permissible wavefront irregularity C: maximum permissible rotationally symmetric wavefront irregularity D: maximum permissible rms wavefront quantity (target subtracted) of type x (x is t: total rms deformation, i: rms irregularity, or a: rms asymmetry) E: reference wavelength (nm) Target: Ci = x i: index of the Zernike polynomial term of the target aberration x: numerical value of the target, in wavelengths unit |

# Collimator Optics Specifications

LGSWFS Collimator Module (COL) consists in a collimator which re-images the telescope’s pupil on the lenslet array.

This section presents the specifications for the 3 lenses, 2 mirrors and Narrow Band Pass Filter inside the collimator assembly (see figure below).

## COL Collimator Optical Assembly

Table 4-1. COL Collimator Prescription

Data in mm, except when unit is indicated, at 20 °C

| Element Name | Radius Curvature | Thickness | Diameter | Material | Tilt | Decenter | Distance |
| --- | --- | --- | --- | --- | --- | --- | --- |
| LGS Image | Plane |  | 21.75 | Air |  |  | -20.00 ± 0.1 |
| Folding Mirror 1 | Plane ± 0.5 fringe | 5.0 ± 0.1 | 42.43x30.0 | S-BSL7 |  |  | 20.00 ± 0.1 |
| Field Stop | Plane |  | 21.75 | Air |  |  | 4.000 ± 0.05 |
| NBP Filter | Plane ± 1.0 fringe | 3.3 ± 0.05 | 30.0 | Borofloat |  |  | 42.98 ± 0.05 |
| Collimator Lens 1 | CX 267.65 ± 0.268 CX 86.901 ± 0.087 | 7.5 ± 0.05 | 40.0 ± 0.02 | S-LAH95 | ± 1’ | ± 0.02 | 1.889 ± 0.02 |
| Collimator Lens 2 | CC 54.564 ± 0.055 CC 67.794 ± 0.068 | 5.0 ± 0.05 | 40.0 ± 0.02 | S-BSL7 | ± 1’ | ± 0.02 | 42.68 ± 0.05 |
| Collimator Lens 3 | Plane ± 1.0 fringe CX 84.342 ± 0.084 | 9.0 ± 0.05 | 54.0 ± 0.02 | S-LAH95 | ± 1’ | ± 0.05 | 81.40 ± 0.05 |
| Folding Mirror 2 | Plane ± 0.2 fringe | 6.0 ± 0.1 | 60.0 | Silica |  |  | 40.00 ± 0.05 |
| MLA Pupil | Plane |  | 22.576 | Image |  |  |  |

COL_NBPF

COL_FM1

COL_FM2

COL_L3

COL_L1

COL_L2

MLA Pupil

Pupil Steering

Device

Field Stop

Figure 4-1. COL Collimator Optical Assembly Drawing

| Full Field Aperture Ø 6.42 ± 0.02 COL_L3 COL_L2 COL_L1 49.2 ± 0.2 121.4 ± 0.1 (66.07) Pupil Aperture 13/ — RMSi < 0.15; λ = 589.3 (∞) 7.69 ± 0.02 Ø 22.58 ± 0.02 P1 Ø 22.58 im |  |  |
| --- | --- | --- |
| Note 1: Drawing intended for opto-mechanical assembly testing Note 2: Focal length (λ = 589.3) 113.35 mm ± 0.2 mm Note 3: Full object space Field of View ± 3.88 ° square Note 4: WFE test object space Field of View ± 2 ° circular Note 5: Image space F/# 5 |  |  |
| Ind. acc. ISO 10110 | Collimator Assembly |  |

λ

COL Collimator Doublet (COL_L1+COL_L2)

| A P1 Ø 36 COL_L2 COL_L1 1.89 ± 0.02 Ø 40 ± 0.02 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Note 1: Drawing intended for mechanical assembly |  |  |  |  |  |
| Surface 1 | Surface 2 |  | Surface 3 |  | Surface 4 |
| λ Øe 36 (SLAR_589) 4/ 1’ | - Øe 36 (SLAR_589) 4/ — |  | λ Øe 36 (VAR_589) 4/ — |  | λ Øe 36 (VAR_589) 4/ 1’ |
| Ind. acc. ISO 10110 |  | Collimator Doublet |  | (COL_L1+COL_L2) |  |

Rq 2

G

COL Collimator Doublet Lens 1 (COL_L1)

| A Ø 40 ± 0.02 7.5 ± 0.05 Rq 0.001 P4 0.002/1.0 Rq 0.001 P4 0.002/1.0 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 267.65 ± 0.268 CX Øe 36 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.040; C3x0.063; L1x0.010; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 86.901 ± 0.087 CX Øe 36 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.040; C3x0.063; L1x0.010; E0.5 |
| Ind. acc. ISO 10110 | Collimator Doublet Lens 1 | COL_L1 |

Rq 2

G

COL Collimator Doublet Lens 2 (COL_L2)

| A Ø 40 ± 0.02 3.05 ± 0.02 Rq 0.001 P4 0.002/1.0 Rq 0.001 P4 0.002/1.0 5 ± 0.05 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.2 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 54.564 ± 0.055 CC Øe 32 λ Protective chamfer 0.4 - 0.6 VAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-BSL7 (Ohara) nd 1.5163 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 67.794 ± 0.068 CC Øe 36 λ Protective chamfer 0.4 - 0.6 VAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | Collimator Doublet Lens 2 | COL_L2 |

## COL Collimator Lens 3 (COL_L3)

| Rq 2 G A Ø 54 ± 0.02 Rq 0.001 P4 0.002/1.0 9 ± 0.05 Rq 0.001 P4 0.002/1.0 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R ∞ Øe 48 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ 1.0 (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 84.342 ± 0.084 CX Øe 48 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | Collimator Lens 3 | COL_L3 |

Rq 2

G

COL Narrow Bandpass Filter (COL_NBPF)

| Ø 30 ± 0.02 Rq 0.002 P3 0.002/1.0 Rq 0.002 P3 0.002/1.0 3.3 ± 0.05 A |  |  |
| --- | --- | --- |
| Note 1: CTE (+20, +300 °C) = 3.25 10-6/°C Note 2: Alternate substrate Fused Silica with thickness adjustment Note 3: Coated transmitted WFE specification: 13/ — RMSi < 0.05; λ = 589.3 (all Ø 10) |  |  |
| Surface 1 | Material specification | Surface 2 |
| R ∞ Øe 27 λ Protective chamfer 0.4 - 0.6 NBP_589_10 Bandpass 3/ 3 (0.5); λ = 632.8 4/ — 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | Borofloat ® (Schott) nd 1.4714 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R ∞ Øe 27 λ Protective chamfer 0.4 - 0.6 NBP_589_10 Blocking 3/ 3 (0.5); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | COL Narrow BP Filter | COL_NBPF |

## COL Folding Mirror 1 (COL_FM1)

| 17 ± 0.05 45 ± 0.017 ° Ø 30 ± 0.05 Rq 0.001 P4 0.002/1.0 A Rq 2 G Rq 2 G |  |  |
| --- | --- | --- |
| Note 1: Incidence angle 45° Note 2: S-BSL7 CTE (-30, +70 °C) = 7.2 10-6/°C, adapted to steering device mount material, Titanium, CTE (+20 °C) = 8.6 10-6/°C Note 3: Drawing is not representative of mechanical design (See mechanical drawing for exact cutting layout) |  |  |
| Surface 1 | Material specification | Surface 2 |
| R ∞ Øe 38 x 27 λ Protective chamfer 0.4 - 0.6 HRD_589_120 3/ 0.5 (0.2); λ = 632.8 4/ — 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-BSL7 (Ohara) 0/ — 1/ — 2/ — | R ∞ Øe — λ Protective chamfer 0.4 - 0.6 — 3/ — 4/ 1’ 5/ — To be cemented |
| Ind. acc. ISO 10110 | COL Folding Mirror 1 | COL_FM1 |

Figure 4-2. COL_FM1 Mechanical Drawing

Rq 2

G

COL Folding Mirror 2 (COL_FM2)

| Ø 60 ± 0.05 9 ± 0.1 Rq 2 G A Rq 0.001 P4 0.002/1.0 |  |  |
| --- | --- | --- |
| Note 1: Incidence angle 45° Note 2: Alternate substrate Zerodur |  |  |
| Surface 1 | Material specification | Surface 2 |
| R ∞ Øe 54 λ Protective chamfer 0.4 - 0.6 HRD_589_120 3/ 0.5 (0.2); λ = 632.8 4/ — 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | Fused Silica 0/ — 1/ — 2/ — | R ∞ Øe — λ Protective chamfer 0.4 - 0.6 — 3/ — 4/ 3’ 5/ — |
| Ind. acc. ISO 10110 | COL Folding Mirror 2 | COL_FM2 |

# Detector Module Relay Optics Specifications

LGSWFS Detector Module (LDM) consists in a lenslet array which samples the telescope’s pupil image and an optical relay which re-images the lenslet array focal plane on the camera detector.

This section presents the specifications for the 6 lenses inside the relay optics (see figure below).

Figure 5-1. Cross-section of a single LDM

## LDM Relay Optical Assembly

Table 5-1. LDM Relay Prescription

Data in mm, except when unit is indicated, at 20 °C

| Element Name | Radius Curvature | Thickness | Diameter | Material | Tilt | Decenter | Distance |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MLA Image | Plane |  | 22.576 | Air |  |  | 8.180 ± 0.05 |
| Relay Lens 1 | CX 81.235 ± 0.081 Plane ± 1.0 fringe | 4.0 ± 0.05 | 31.2 ± 0.02 | S-LAH95 | ± 1’ | ± 0.05 | 59.93 ± 0.02 |
| Relay Lens 2 | CX 38.847 ± 0.039 Plane ± 1.0 fringe | 4.2 ± 0.05 | 25.0 ± 0.02 | S-LAH95 | ± 1’ | ± 0.02 | 3.255 ± 0.02 |
| Relay Lens 3 | CX 13.426 ± 0.013 CC 8.924 ± 0.009 | 6.8 ± 0.02 | 22.0 ± 0.02 | S-LAH95 | ± 1’ | ± 0.01 | 3.936 ± 0.01 |
| Diaphragm | Plane |  | 9.7 | Air |  |  | 6.796 ± 0.01 |
| Relay Lens 4 | CC 8.353 ± 0.008 CX 13.263 ± 0.013 | 6.8 ± 0.02 | 22.0 ± 0.02 | S-LAH95 | ± 1’ | ± 0.01 | 2.671 ± 0.02 |
| Relay Lens 5 | Plane ± 1.0 fringe CX 35.233 ± 0.035 | 4.8 ± 0.05 | 27.0 ± 0.02 | S-LAH95 | ± 1’ | ± 0.02 | 2.455 ± 0.02 |
| Relay Lens 6 | CX 43.482 ± 0.043 Plane ± 1.0 fringe | 4.2 ± 0.05 | 27.0 ± 0.02 | S-LAH95 | ± 1’ | ± 0.05 | 5.474 |
| Cam. Interface | Plane |  | 25.0 | Air |  |  | 11.53 |
| Camera Window | Plane Plane | 1.0 | 25.4 | Silica |  |  | 3.0 |
| Detector Window | Plane Plane | 0.5 | 21.6 | Index 1.5 |  |  | 1.5 |
| Detector | Plane |  | 9.792 | Image |  |  |  |

LDM_L6

LDM_L5

LDM_L4

LDM_L3

LDM_L2

LDM_L1

Diaphragm

MLA

Detector

Det Window

Cam Window

Cam Interface

Figure 5-2. LDM Optical Assembly Drawing

- Relay Lens 6 axial position is tunable with shims, to adjust magnification on detector.

- Camera axial position is tunable with fine pitch screws, to adjust focus on detector.

| Image Field Aperture 13/ — RMSi < 0.12; λ = 589.3 im Oversized Pupil Aperture LDM_L61 Object Field Aperture 7.43 ± 0.02 Ø 4.90 ± 0.01 Ø 1.39 ± 0.01 Ø 6.42 ± 0.02 Ø 22.58 ± 0.02 LDM_L11 LDM_L41 LDM_L51 LDM_L2 LDM_L3 (109.84) 8.18 ± 0.05 22.5 ± 0.1 ob |  |  |
| --- | --- | --- |
| Note 1: Drawing intended for opto-mechanical assembly testing Note 2: Magnification (λ = 589.3) 1:2.3056 mm (adjustment with LDM_L6 shimming) Note 3: Object space Field of View ± 11.29 mm circular Note 4: Telecentric object space F# 6.454 x 6.454 square Note 5: Image space grid distortion < ± 4.3 µm |  |  |
| Ind. acc. ISO 10110 | LDM Relay Assembly |  |

Rq 2

G

LDM Relay Lens 1 (LDM_L1)

| A Ø 31.2 ± 0.02 Rq 0.001 P4 0.002/1.0 Rq 0.001 P4 0.002/1.0 4 ± 0.05 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 81.235 ± 0.081 CX Øe 28 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.040; C3x0.063; L1x0.010; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 1x0.100 2/ — | R ∞ Øe 28 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ 1.0 (0.4); λ = 632.8 4/ 1’ 5/ 3x0.040; C3x0.063; L1x0.010; E0.5 |
| Ind. acc. ISO 10110 | LDM Relay Lens 1 | LDM_L1 |

Rq 2

G

LDM Relay Lens 2 (LDM_L2)

| A Rq 0.001 P4 0.002/1.0 Rq 0.001 P4 0.002/1.0 4.2 ± 0.05 Ø 25 ± 0.02 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 38.847 ± 0.039 CX Øe 22 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R ∞ Øe 22 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ 1.0 (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | LDM Relay Lens 2 | LDM_L2 |

## LDM Relay Lens 3 (LDM_L3)

| A Rq 2 G Rq 0.001 P4 0.002/1.0 Rq 0.001 P4 0.002/1.0 Rq 2 G B 3.94 ± 0.02 Ø 22 ± 0.02 6.8 ± 0.02 (10.74 ± 0.02) |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 13.426 ± 0.013 CX Øe 20 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 8.924 ± 0.009 CC Øe 13 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’; 1’ AB 5/ 2x0.100; C2x0.160; L2x0.016; E0.5 |
| Ind. acc. ISO 10110 | LDM Relay Lens 3 | LDM_L3 |

## LDM Relay Lens 4 (LDM_L4)

| A Rq 2 G Rq 0.001 P4 0.002/1.0 6.8 ± 0.02 Rq 2 G Rq 0.001 P4 0.002/1.0 4.48 ± 0.02 B Ø 22 ± 0.02 (11.28 ± 0.02) |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 8.353 ± 0.008 CC Øe 13 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’; 1’ AB 5/ 2x0.100; C2x0.160; L2x0.016; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 13.263 ± 0.013 CX Øe 20 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | LDM Relay Lens 4 | LDM_L4 |

Rq 2

G

LDM Relay Lens 5 (LDM_L5)

| A Rq 0.001 P4 0.002/1.0 Rq 0.001 P4 0.002/1.0 4.8 ± 0.05 Ø 27 ± 0.02 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R ∞ Øe 24 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ 1.0 (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 35.233 ± 0.035 CX Øe 24 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | LDM Relay Lens 5 | LDM_L5 |

Rq 2

G

LDM Relay Lens 6 (LDM_L6)

| A Rq 0.001 P4 0.002/1.0 Rq 0.001 P4 0.002/1.0 4.2 ± 0.05 Ø 27 ± 0.02 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.3 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 43.482 ± 0.043 CX Øe 24 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ — (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-LAH95 (Ohara) nd 1.9037 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R ∞ Øe 24 λ Protective chamfer 0.4 - 0.6 SLAR_589 3/ 1.0 (0.4); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | LDM Relay Lens 6 | LDM_L6 |

# Calibration Unit Optics Specifications

LGSWFS Calibration Unit Module (CAL) consists in a lenslet array which samples the telescope’s pupil image and an optical relay which re-images the lenslet array focal plane on the camera detector.

This section presents the specifications for the 2 doublets, the pupil mask plate and the folding mirror inside the Calibration Unit optics (see figure below).

## CAL Relay Optical Assembly

Table 6-1. CAL Calibration Unit Prescription

Data in mm, except when unit is indicated, at 20 °C

| Element Name | Radius Curvature | Thickness | Diameter | Material | Tilt | Decenter | Distance |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Source Object | Plane |  | 1.408 | Air |  |  | 95.79 ± 0.1 |
| Doublet 1 Lens 2 | CX 92.005 ± 0.092 CC 37.998 ± 0.038 | 3.0 ± 0.05 | 30.0 ± 0.02 | S-TIM25 | ± 1’ | ± 0.02 | Cemented |
| Doublet 1 Lens 1 | CX 37.998 ± 0.038 CX 74.210 ± 0.074 | 8.0 ± 0.05 | 30.0 ± 0.02 | S-BSL7 | ± 1’ | ± 0.02 | 96.97 ± 0.05 |
| Pupil Mask | Plane |  | 20.0 ± 0.01 | Black Cr |  | ± 0.01 | Deposited |
| Pupil Mask Plate | Plane ± 1.0 fringe Plane ± 1.0 fringe | 4.0 ± 0.05 | 30.0 ± 0.02 | Silica | ± 1’ | ± 0.02 | 50.23 ± 0.05 |
| Folding Mirror | Plane ± 0.2 fringe | 5.0 ± 0.05 | 40.0 ± 0.05 | Silica |  |  | 44.0 ± 0.05 |
| Doublet 2 Lens 1 | CX 74.210 ± 0.074 CX 37.998 ± 0.038 | 8.0 ± 0.05 | 30.0 ± 0.02 | S-BSL7 | ± 1’ | ± 0.02 | Cemented |
| Doublet 2 Lens 2 | CC 37.998 ± 0.038 CX 92.005 ± 0.092 | 3.0 ± 0.05 | 30.0 ± 0.02 | S-TIM25 | ± 1’ | ± 0.02 | 95.79 ± 0.1 |
| CAL Image | Plane |  | 1.408 | Image |  |  |  |

CAL_FM

Doublet 1

(CAL_L1+CAL_L2)

Doublet 2

(CAL_L1+CAL_L2)

Pupil Mask

(CAL_PM)

To Image

Source

Figure 6-1. CAL Calibration Unit Optical Assembly Drawing

| 95.79 ± 0.1 (55.0) CAL_FM1 13/ — RMSi < 0.07; λ = 589.3 Ø 5.74 ± 0.01 Ø 20 ± 0.01 Image Field Aperture Ø 1.41 ± 0.01 Object Field Aperture Ø 1.41 ± 0.01 Pupil Aperture CAL_PM1 CAL_L1 CAL_L2 (162.2) CAL_L11 CAL_L2 95.79 ± 0.1 im ob |  |  |
| --- | --- | --- |
| Note 1: Drawing intended for opto-mechanical assembly testing Note 2: Unit Magnification (λ = 589.3) Note 3: Object space Field of View Ø 2.5 mm Note 4: Telecentric object / image spaces F# 5 |  |  |
| Ind. acc. ISO 10110 | Calibration Unit Assembly |  |

λ

CAL Cemented Doublet (CAL_L1+CAL_L2)

| A Ø 30 ± 0.02 P1 Ø 27 CAL_L1 CAL_L2 13/ — RMSi < 0.032 (all Ø 20); λ = 632.8 (∞) im |  |  |
| --- | --- | --- |
| Note 1: Focal length [(λ = 632.8) 100.06 mm; (λ = 589.3) 100.03 mm] ± 0.2 mm |  |  |
| Surface 1 | Surface 2 | Surface 3 |
| - Øe 27 (VAR_589) 4/ 1’ | λ Øe 27 — 4/ Δ 0.2’ Cement: NOA61 (10 µm) | λ Øe 27 (VAR_589) 4/ 1’ |
| Ind. acc. ISO 10110 | CAL Cemented Doublet | (CAL_L1+CAL_L2) |

### CAL Cemented Doublet Lens 1 (CAL_L1)

| Rq 2 G A Ø 30 ± 0.02 8 ± 0.05 Rq 0.002 P3 0.002/1.0 Rq 0.002 P3 0.002/1.0 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.2 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 74.210 ± 0.074 CX Øe 27 λ Protective chamfer 0.4 - 0.6 VAR_589 3/ — (0.5); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | S-BSL7 (Ohara) nd 1.5163 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 37.998 ± 0.038 CX Øe 27 λ Protective chamfer 0.4 - 0.6 — 3/ — (0.5); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 To be cemented |
| Ind. acc. ISO 10110 | CAL Doublet Lens 1 | CAL_L1 |

Rq 2

G

CAL Cemented Doublet Lens 2 (CAL_L2)

| A Ø 30 ± 0.02 Rq 0.002 P3 0.002/1.0 3 ± 0.05 Rq 0.002 P3 0.002/1.0 |  |  |
| --- | --- | --- |
| Note 1: Radii of curvature and thickness will be adjusted to glass melt data and manufacturer test plates Note 2: CTE (-30, +70 °C) = 7.9 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R 37.998 ± 0.038 CC Øe 27 λ Protective chamfer 0.4 - 0.6 — 3/ — (0.5); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 To be cemented | S-TIM25 (Ohara) nd 1.6727 ± 0.0005 νd — 0/ 10 1/ 3x0.100 2/ — | R 92.005 ± 0.092 CX Øe 27 λ Protective chamfer 0.4 - 0.6 VAR_589 3/ — (0.5); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | CAL Doublet Lens 2 | CAL_L2 |

## CAL Pupil Mask (CAL_PM)

Rq 2

G

CAL Pupil Mask Plate

| Pupil Mask Ø 20 Ø 30 ± 0.02 A Rq 0.002 P3 0.002/1.0 4 ± 0.05 Rq 0.002 P3 0.002/1.0 |  |  |
| --- | --- | --- |
| Note 1: CTE (-30, +70 °C) = 0.5 10-6/°C |  |  |
| Surface 1 | Material specification | Surface 2 |
| R ∞ Øe 20 λ Protective chamfer 0.4 - 0.6 VAR_589 + BCR_589 3/ 1 (0.5); λ = 632.8 4/ — 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | Fused Silica nd 1.4585 ± 0.0002 νd — 0/ 10 1/ 3x0.100 2/ — | R ∞ Øe 20 λ Protective chamfer 0.4 - 0.6 VAR_589 3/ 1 (0.5); λ = 632.8 4/ 1’ 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 |
| Ind. acc. ISO 10110 | CAL Pupil Mask Plate | CAL_PM |

### CAL Pupil Mask Shape

| λ VAR_589 Ø 0.4 ± 0.01 Ø 30 ± 0.02 λ BCR_589 Ø 5.68 ± 0.01 Ø 20 ± 0.01 |  |  |
| --- | --- | --- |
| Ind. acc. ISO 10110 | CAL Pupil Mask Shape | CAL_PM |

Rq 2

G

CAL Folding Mirror (CAL_FM)

| Ø 40 ± 0.05 6 ± 0.1 Rq 2 G A Rq 0.001 P4 0.002/1.0 |  |  |
| --- | --- | --- |
| Note 1: Incidence angle 45° Note 2: Alternate substrate Zerodur |  |  |
| Surface 1 | Material specification | Surface 2 |
| R ∞ Øe 36 λ Protective chamfer 0.4 - 0.6 HRD_589_120 3/ 0.5 (0.2); λ = 632.8 4/ — 5/ 3x0.100; C3x0.160; L3x0.016; E0.5 | Fused Silica 0/ — 1/ — 2/ — | R ∞ Øe — λ Protective chamfer 0.4 - 0.6 — 3/ — 4/ 3’ 5/ — |
| Ind. acc. ISO 10110 | CAL Folding Mirror | CAL_FM |

# Annex

## Coatings preliminary Design

These designs are only informative and used as tentative designs for defining the specifications.

They are marginally optimized and could be improved.

Layers materials: (QWOT, Quarter Wave Optical Thickness at CWL, Center Wavelength)

H:		TiO2 (n @589 = 2.3588)	L:	SiO2 (n @589 = 1.4526)

N:		MgF2 (n @589 = 1.3777)	R:	Cr (n @589 = 3.3781)

### SLAR_589 Coating Design

S-LAH95 | N | Air

CWL 589 nm, 1 layer, 107 nm total thickness, T @589 = 99.9998 %

### VAR_589 Coating Design

Silica | 1.76H 0.64L | Air

CWL 589 nm, 2 layers, 175 nm total thickness, T @589 = 99.9985 %

### NBP_589_10 (Bandpass + Blocking) Coating Design

Bandpass: Silica | 1.76H 0.64L | (HL)2 2H (LH)2 L (HL)3 2H (LH)3 L (HL)2 2H (LH)2 | Air

CWL 589 nm, FWHM 10.6 nm, 35 layers, 3045 nm total thickness, T1 @589 = 99.9985 %

Blocking: Silica | 1.76H 0.64L | 0.74 (0.5H L 0.5H)14 1.38 (0.5L H 0.5L)14 | Air

CWL 589 nm, 60 layers, 5036 nm total thickness, T2 @589 = 99.8717 %

Total: T @589 = T1 T2 = 99.85 %, Ghost level @589 = R1 R2 = 1.925e-6 %

Figure 7-1. NBP Filter Coating Simulations Transmission

### HRD_589_120 Coating Design

Silica | 0.59H 0.77L 1.25H 0.74L (HL)11 0.64H 2.21L | Air

CWL 639 nm, 28 layers, 2542 nm total thickness, R @589 = 99.9946 %

### BCR_589 Coating Design

Silica | 4.00R 0.53H 1.58L 0.70H 1.94L | Air

CWL 589 nm, 5 layers, 608 nm total thickness, T @589 = 0.000011 %, R @589 = 0.0045 %

Figure 7-2. BCR Coating Simulations Transmission / Total Optical Density

### Total LGS WFS Coatings Transmission

| Coating Name | Number | Components COL + LDM (CAL) |
| --- | --- | --- |
| SLAR_589 | 16 | COL_L1, COL_L3 LDM_L1, LDM_L2, LDM_L3, LDM_L4, LDM_L5, LDM_L6 |
| VAR_589 | 4 (+4) | COL_L2, LDM_MLA* (CAL_L1, CAL_L2, CAL_PM) |
| NBP_589_10 | 1 | COL_NBPF |
| HRD_589_120 | 2 (+1) | COL_FM1, COL_FM2 (CAL_FM) |
| BCR_589 | 0 (+1) | (CAL_PM) |

(*) LDM_MLA not included in this specifications document

- LGS Probe: TLGS = TNBP RHRD2 TVAR4 TSLAR16 (TLGS @589 = 99.85 %)

- Calibration Unit: TCAL = RHRD TVAR4 (TCAL @589 = 99.99 %)

Figure 7-3. LGS Probe Coatings Simulations Transmission / Total Optical Density

Figure 7-4. Calibration Coatings Simulations Transmission / Total Optical Density

** End of document ***